## Slide 1: Dr. Eduard Aleksanyan
2026-05-16, DILIJAN
Perovskite research at
ADVANCED THIN FILM DEPOSITION AND CHARACTERISATION LABORATORY
A. Alikhanyan National Science Laboratory,
Applied Physics Research Division
Head of Optical Spectroscopy group

## Slide 2
Milestones in PSC Research
2018
2019
2020
2021
2022
2024
2025
Start of perovskite research
First synthesis of perovskites via ball milling, Improvement of Stability
Initiation of radiation damage studies
Development of perovskite thin films by PVD
Introduction of spin coating technique
First working semitransparent solar cell fabricated in ambient air
First working flexible perovskite solar cell
aeduard@yerphi.am
2026
2028
20XX
First working perovskite based LED
Upscaling
Market entry
2029
Tandems
2026-05-16, DILIJAN

## Slide 3
Proton irradiation at cyclotrone C18
Proton energy – up to 18 MeV (1.4 MeV, 6.0 MeV, 9.0 MeV, 12.5 MeV, 15.5 MeV)
Doses – 1014 p/cm2, 2 x 1014 p/cm2, 5 x 1014 p/cm2, 1015 p/cm2, 5 x 1015 p/cm2 (Current – 1-5 μA)
e.aleksanyan@ysu.am
2026-05-14, YSU

## Slide 4
Heating effect on CsPbBr3
55 oC
450 oC
500 oC
350 oC
527 oC
600 oC
550 oC
aeduard@yerphi.am
2026-05-16, DILIJAN

## Slide 5
EDS mapping of CsPbBr3
aeduard@yerphi.am
2026-05-16, DILIJAN

## Slide 6
Spin Coating
Cutting and cleaning of Glass/FTO or PET-ITO substrates
Spin Coating of c-TiO2 and mp-TiO2
Spin Coating of hybrid perovskite
Spin coating of HTL
Au deposition through magnetron sputtering / thermal evaporation
Measurements and evaluation
Glass
FTO
TiO2
Perovskite
HTL
Au/Ag
Cs0.04(FA0.87MA0.13)0.96Pb(I0.7Br0.3)3
aeduard@yerphi.am
2026-05-16, DILIJAN

## Slide 7
Perovskite solar cell production
10x10 cm Glass/FTO
Cut to 2.5 x 2.5cm
Washing
Spin coating of c-TiO2
Spin coating of mp-TiO2
CBD of blocking layer
Preparation fo Perovskite solution
Deposition of Pe and HTL
PVD of top Au contact
Final structure of PSC
Semitransparent solar cell
Solar simulator
I-V and PCE
Optical transmission
aeduard@yerphi.am
2026-05-16, DILIJAN

## Slide 8
Hot injection
Synthesis of CsPbI3 and CsPbBr3 nanoparticles
TEM image of nanoparticles
aeduard@yerphi.am
2026-05-16, DILIJAN

## Slide 9
Photoluminescence in perovskites, PeLEDs
The emission from CsPbX3 (X=I, Br, Cl) covers the whole visible range from 400-730
Traditional organic light-emitting diodes (OLEDs, FWHM~ 40 nm)
For perovskites this value is ~15nm
It can solve the red deficiency problem for warm white lighting source.
aeduard@yerphi.am
2026-05-16, DILIJAN

## Slide 10
Temperature dependence of CsPbBr3 PL
Unlike conventional semiconductors, lead halide perovskites often exhibit anomalous PL red shift upon cooling due to strong electron–phonon coupling
aeduard@yerphi.am
2026-05-16, DILIJAN

## Slide 11
Perovskite based LEDs
Solar Cell
LED
n-i-p structure
p-i-n structure
aeduard@yerphi.am
2026-05-16, DILIJAN

## Slide 12
Upgrade of our lab
All fabrication steps of the perovskite solar cell are carried out in an inert atmosphere.
aeduard@yerphi.am
2026-05-16, DILIJAN
H2O and O2 < 0.1ppm

## Slide 13
Upscaling
aeduard@yerphi.am
2026-05-16, DILIJAN
Blade coating
Magnetron sputtering
Interdigitated contacts for transparency improvement

## Slide 14
NanoEnergy
Elbak Elbakyan
Founder of NanoEnergy
Eduard Aleksanyan
Head of R&D
Karen Zakaryan
Head of Production
NanoEnegy Solar Panels https://nanoenergy.io
info@nanoenergy.io
2026-05-16, DILIJAN

## Slide 15
Research team
Eduard Aleksanyan - Dr., A. Alikhanyan National Laboratory (Yerevan Physics Institute) foundation
Artur Papikyan - PhD., A. Alikhanyan National Laboratory (Yerevan Physics Institute) foundation
Anush Badalyan – Dr., A. Alikhanyan National Laboratory (Yerevan Physics Institute) foundation
Arevik Arestakyan – Master, A. Alikhanyan National Laboratory (Yerevan Physics Institute) foundation
Hrant Yeritsyan – Student at YSU
Arman Hovhannisyan – Student at YSU
Norik Grigoryan – Dr., A. Alikhanyan National Laboratory (Yerevan Physics Institute) foundation
Artavazd Kirakosyan - Dr., Chungnam National University, Korea
aeduard@yerphi.am
2026-05-16, DILIJAN

## Slide 16
Collaboration
aeduard@yerphi.am
2026-05-16, DILIJAN

## Slide 17
Thank You !!!
aeduard@yerphi.am
2026-05-16, DILIJAN

## Slide 18
What are Perovskites
e.aleksanyan@ysu.am
2026-05-14, YSU
ABX3 – perovskite structure (CaTiO3, YAlO3, MgSiO3, BaTiO3, etc.)
MAPbX3, (MA) = CH3NH3+
FAPbX3, (FA) = CH(NH2)2+
CsPbX3
Direct bandgap
  Thin film devices
Tunable bandgap
  Lighting, LEDs
Low temperature processing
    Low production cost
    Abundant materials (resource efficient)
Tsutomu MIYASAKA
2009
Henry J Snaith
2013
X = I, Br, Cl

## Slide 19
National Renewable Energy Laboratory Results - 2026
e.aleksanyan@ysu.am
2026-05-14, YSU

## Slide 20
forming nanocrystals
surface functionalization
compositional tuning
Lead Halide Perovskite – Pros and Cons
Suitable characteristics of LHP material
Simple manufacturing process
Low cost
Defect tolerance
Challenges for LHP
Stability in ambient environment (effective luminescence can only occur in cubic phase)
Intrinsic toxicity
WE NEED TO STABILIZE HIGH-PERFORMANCE PHASE
2026-05-14, YSU

## Slide 21
Solar absorption and perovskite phases
e.aleksanyan@ysu.am
2026-05-14, YSU
α - CsPbI3 - Eg = 1.73 eV
δ - CsPbI3 - Eg = 2.75 eV
t < 0.8 => orthorhombic
0.8 < t < 1 => cubic
t > 1 => hexagonal
for CsPbI3 – t=0.82
ABX3 – tolerance factor
Cubic CsPbI3 (Eg = 1.73 eV)  orthorhombic nonperovskite phase (Eg = 3.01 eV)

## Slide 22
Perovskites Synthesis by Mechanochemistry
CsI+PbI2=CsPbI3
CsBr+PbI2=CsPbI2Br
CsBr+PbBr2=CsPbBr3
CsI+PbI2+NdI3=CsPbI3:Nd
CsBr+PbBr2+KI=CsPbI3+KBr
…
T = 77K, 300K
t = 5 min, 25 min, 1h, 2h
No extra heat, no solvent, high quantities, control, rapid, phase pure,
The elimination of non-radiative recombination pathways by passivation of traps (The passivation using KI)
Nd3+ ions have been successfully incorporated into host CsPbI3 lattice
e.aleksanyan@ysu.am
2026-05-14, YSU

## Slide 23
Material Synthesis
Nd stabilization vs Br stabilization
CsPbI3 with Br
0 -> 30 min
CsPbI3 with Nd3+
0 -> 20 hours
Apart from decreasing the Pb concentration, doping LHP with Nd improves the stability and introduces additional PL emission lines
e.aleksanyan@ysu.am
2026-05-14, YSU
Notes: Add pressure effects
Add ATFDCL logo
Add nanomaterials and hot injection
Add SEM t-dependence video
Add TEM sample preparation video
Add ND and CNU campuses

## Slide 24
Pressure induced phase stabilization (formation ???)
10t, 25t
δ-CsPbI3
α-CsPbI3
2026-05-14, YSU

## Slide 25
Material Synthesis
CsBr (Alfa Aesar 99%) and PbBr2 (Alfa Aesar 98+%)
Double source vapor deposition
Glass substrate (76 x 25 x 1.06 mm)
Vacuum ≤ 10-4 Torr
Rotating substrate
No heating during deposition
Annealed at 100°C, ~1 h
To have identical samples, a big sample was deposited and cut into 10 pieces
PVD method
Vacuum
Substrate
Crucibles
Initials
Sample
e.aleksanyan@ysu.am
2026-05-14, YSU