## Slide 1
ԴԻԼԻՋԱՆ 2026
Առաջադեմ նյութերի հենքով միկրո/նանո-էլեկտրամեխանիկական համակարգերի (ՄԷՄՀ/ՆէՄՀ) նախագծում և պատրաստում
ՔՖԻ “Նանոգիտության և տեխնոլոգիաների նորարարական կենտրոն” գիտահետազոտական լաբորատորիայի վարիչ։
ԵՊՀ կոնդենսացված վիճակի ֆիզիկայի գիտական կենտրոնի ավագ գիտաշխատող
ԵՊՀ կոնդենսացված վիճակի ֆիզիկայի ամբիոնի դասախոս
ԱՌԱՋԸՆԹԱՑ ԱՐԴՅՈՒՆԱՎԵՏ ԳԻՏՈՒԹՅԱՄԲ 2026
Մկրտիչ Երանոսյան

## Slide 2
Մեր լաբորատորիան
ՆՏՆ կենտրոնի աշխատակիցների ընդհանուր թիվը 23 է, որից
2-ը մինչև 40 տարեկան գիտաշխատողներ են,
8-ը մինչև 30 տարեկան երիտասարդ գիտաշխատողներ,
2-ը մագիստրատուրայի ուսանողներ,
4-ը բակալավրիատի ուսանողներ,
2-ը ավագ ճարտարագետներ
1-ը ավագ գիտաշխատող

## Slide 3
Mkrtich Yeranosyan
Head of Laboratory PhD
Razmik Navoyan
Avetis Simonyan PhD
Erik Vahanyan
Hayk Hovhannisyan
Heriqnaz Asatryan
Aram Qerobyan
Armen Petrosyan PhD
Mkrtich Asatryan

## Slide 4: Rsearch group of Nano-Biocensorics
Astghik
PhD student (Chemistry) Local Coordinator
Vardan
PhD candidate (Chemistry)
Research Mentor
Derenik
MCs student (Radiophysics)
Device engineer-technician
Diana
BSc student (Biochemistry)
Laboratory assistant
Lusine
PhD student (Biology)
Laboratory experimentalist
Nelli
MSc student (Data Science)
Data analyst
Karen
PhD student (Physics)
Theoretical modelling

## Slide 5
Pioneer 180 PLD System
Plasma-enhanced CVD System
EBL Electron beam lithography
Thermal CVD System
ՀՀ ԳԱԱ Ա․Բ․ Նալբանդյանի անվան քիմիական ֆիզիկայի ինստիտուտ
ICNT acquires state-of-the-art devices and equipment
Mask aligner & UV exposure system
RF & DC magnetron sputtering

## Slide 6
LabRAM Nano AFM-Raman (TERS System)
CIMPS-QE/IPCE -UV Photovoltaic/Photoelectrochemical System
Characterization Technologies of Nanosystems
ՀՀ ԳԱԱ Ա․Բ․ Նալբանդյանի անվան քիմիական ֆիզիկայի ինստիտուտ
ZYGO NEW VIEW 7100
Non-contact optical surface profiler
Litesizer 500
Dynamic Light Scattering

## Slide 7
The construction of the Clean Room is in progress (ISO 8 to ISO 5 class, with an area of 120 m2)․

## Slide 8
Six members of our group have completed an internship at the CEITECH Nano Center.

## Slide 9
Նախագծի նպատակը և խնդիրները
Նախագիծը նվիրված է առաջադեմ նյութերով ինտեգրված միկրո/նանո-էլեկտրամեխանիկական համակարգերի (ՄԷՄՀ/ՆԷՄՀ) ստացմանը, բնութագրմանը և դրանց հենքի վրա նանո-բիոսենսորների նախագծմանը և պատրաստմանը։
ՄԷՄՀ/ՆԷՄՀ տեխնոլոգիաները համատեղում են էլեկտրոնային և մեխանիկական տարբեր բաղադրիչներ միևնույն մանրաչափային ինտեգրալային հարթակում՝ ապահովելով բարձր զգայունություն, արագագործություն և էներգիարդյունավետություն։
Այդպիսի համակարգերից են նանո-բիոսենսորները, որոնք կարող են հայտնաբերել առանձին մոլեկուլներ, և պահանջված են բժշկական ախտորոշման և շրջակա միջավայրի մոնիտորինգի գործում։
Նախագծի շրջանակներում ՄԷՄՀ/ՆԷՄՀ տեխնոլոգիաների բնութագրերի բարելավման նկատառումով՝ մեր կողմից դիտարկվում են հետևյալ առաջադեմ 2D նյութերի՝
գրաֆեն, ածխածնային նանոխողովակներ (CNT),
մոլիբդենի դիսուլֆիդ (MoS₂)
վոլֆրամի դիսուլֆիդ (WS₂)
ինչպես նաև մեկուսիչ նյութերի՝ հեքսագոնալ բորի նիտրիդ (H-BN), սիլիցիումի երկօքսիդ (SiO₂), հաֆնիումի երկօքսիդ (HfO₂) և ալյումինի եռօքսիդ (Al₂O₃), ստացման, բնութագրման և դրանց հենքի վրա նանո-բիոսենսորների պատրաստման հնարավորությունները։

## Slide 10
Thermal and Plasma-Enhanced CVDs

## Slide 11: MoS2 ատոմական շերտերի ստացում CVD եղանակով
Օպտիմալացված պայմաններում E12g (384.7 սմ-1) և A1g (404 սմ-1) A1g-E12g գագաթների միջև տարբերությունը կազմում է 19.3 սմ-1, ինչը վկայում է MoS2 մոնոշերտ բյուրեղի առաջացման մասին, իսկ եռանկյուն միաշերտ բյուրեղները հասնում են 40-50 մկմ չափերի:

## Slide 12: MoS2 flake CVD synthesis

## Slide 13: Ածխածնային նանոխողովակների ստացում CVD եղանակով
Արդյունքները ընդգծում են կատալիզատորի կազմի և սինթեզի տեխնոլոգիական պարամետրերի ազդեցությունը ԱՆԽ-ների արդունավետ ձևավորման և որակի օպտիմալացման գործում: FeMo/MgO կատալիզատորը ցուցաբերել է բարձր կայունություն՝ նպաստելով նանոխողովակների երկարատև աճին՝ արդյունաբերական կիրառությունների համար զգալի մասշտաբայնացման ներուժով:

## Slide 14
CVD պրոցեսի զարգացում «In-situ» ԻԿ սպեկրաչափական եղանակով Art-Photonics
Fig. 5 Heatmap for methane band taken from 1000 to 1500

## Slide 15
Novel observation of SEIRA and SERS in aluminum-doped ZnO–BSA protein corona complexes

## Slide 16: Synthesis, solution-based reflux method
ZnO
AZO

## Slide 17: Synthesis and Characterization of Al-Doped ZnO Nanoparticles
LSPR peak
Notes: AZO , remove (2)
New scale for TEM
Remove the small XRD zoom-in
The shift shows that the doing has occurred, Zn sp3 hybridization , the distance is 23,1 eV, which shows there is no new phase in the system.

## Slide 18
The AFM images display the spherical self-assembled AZO nanoparticles (a) and AZO-BSA protein corona complexes (b, c), as well as cross section profile (d) of the line on the (c).

## Slide 19: Dynamics of BSA Fluorophore Quenching and Molecular Interaction Dynamics
Zeta potential and hydrodynamic diameter change
Zeta potential | Zeta potential | Hydrodynamic diameter
AZO | 28 mV | 131 nm
BSA | -0.8 mV | 28 nm
AZO-BSA | -20 mV | 238 nm
Quenching of the BSA fluorescence
Litesizer 500
Dynamic Light Scattering
Notes: - The BSA Fluorescence is mainly dominated with Tryptophan (Trp) residue fluorescence which peaks at 340 nm.
- The Fluorescence of Trp is quenched as AZO concentration is added, because of the complex formation, the Trp goes to its ground state , and doesn’t emit fluorescence after that.

## Slide 20: Spectroscopic Analysis of AZO-BSA Complexes: FTIR Observations
Amide I
Amide II
Astghik S. Tsokolakyan, Vardan A. Hayrapetyan, Heriqnaz V. Asatryan, Avetis S. Simonyan, Alexandr Dejneka, Mkrtich A. Yeranosyan // Novel observation of SEIRA and SERS in aluminum-doped ZnO–BSA protein corona complexes / Optical Materials, 2026, 174, 118036. Q1, IF=4.2
Notes: FT IR spectra
- amide 1 peak is around - around 1650 cm-1
- amide 2 peak is around 1550 cm-1
We can see from the FT IR that the BSA –AZO (with 1 mg/ml BSA) displayed stronger amide peaks than the pure BSA (1 mg/mL)
Here the enhancement factor was around 4.5 : absorbance (BSA 1– blue color)/absorbance (BSA 2 – red color)
AZO-BSA Concentrations
- Here we can see that varying BSA concentrations were added to the AZO and compared to the 1 mg/mL (10-6M) BSA
As we can see the 0.1 mg/mL from AZO - BSA is around same intensity as the 1 mg/mL pure BSA, which means that there is 10 fold enhancement
The same 10x enhancement factor was observed for 0.5 mg/mL (BSA) AZO-BSA and 1 mg/mL (BSA) AZO-BSA as compared to their pure BSA controls
By controlling the experiments higher enhancement factor of 10x was achieved
The FT IR spectra was obtained by drop casting on CaF2 window (20 uL drops)

## Slide 22
Plasma shapes at various pulse energies and process pressures
50mtorr
100 mTorr
150 mTorr
250 mJ
400 mJ
50mtorr
100mtorr
150mtorr

## Slide 23: AFM-SEM

## Slide 24
50 mTorr, 250 mJ
100 mTorr, 250 mJ
150 mTorr, 250 mJ
50 mTorr, 400 mJ
100 mTorr, 400mJ
150 mTorr 400mJ

## Slide 25
Rmax | 123.165 nm
Ra | 1.235 nm
Rq | 2.591 nm
Rtm | 46.255 nm
Rz | 69.194 nm
R3z | 52.585 nm
H | 3.688 nm
Rsk | -9.86
Rku | 243.95
Wmax | 20.744 nm
Wa | 0.962 nm
Wq | 1.281 nm
Imax | 1059 nm
Ia | 4.253 nm
Iq | 20.354 nm
Area | 469um x 352um

## Slide 27
Օպտիկական բազմաշերտ ֆիլտր
nBK7
SiO2
TiO2
SiO2
TiO2
SiO2
TiO2
22 շերտ

## Slide 28
C4D Սենսորներ
Անհպում Չափումներ
Capacitively Coupled Contactless Conductivity Detection (C4D) տեխնոլոգիան թույլ է տալիս իրականացնել բարձր ճշգրտության էլեկտրահաղորդականության չափումներ՝ առանց էլեկտրոդների և հեղուկի անմիջական շփման:
Մաքուր Միջավայր:Պատրաստված է CEITEC Nano RI-ի ISO 5 կարգի մաքուր սենյակներում:
Նյութագիտություն: Սենսորների պատրաստման ծախսատարության նվազեցում՝ հրաժարվելով ազնիվ մետաղների (Au, Pt) կիրառումից:
Կայունություն: Դիէլեկտրիկ շերտը բացառում է կոռոզիան և աղտոտումը:
HfO2
SiO2
Ni
SiO2 – 500 nm
Si – 575 um
145 nm Ni 5nm Cr
HfO2- 60nm
Սենսորի լայնական կտրվածքը
Սենսորի երկրաչափությունը
Սենսորի ֆոտոպատկերը

## Slide 29
Պատրաստման գործընթացը CEITEC-ում
Հիմքի նախապատրաստում
500նմ SiO2
Ֆոտոլիթոգրաֆիա դրական ֆոտոռեզիստ AZ514h
Պլազմային փորագրում (RIE) Անիզոտրոպ փորագրում 150նմ
Մետաղների նստեցում 5nm Cr / 145nm Ni
Ֆոտոռեզիստի հեռացում
Կոնտակտների ծածկում
Ատոմաշերտային նստեցում (ALD) 60 nm HfO2
Մոդելի կառուցում MicroWriter 3 DWL

## Slide 30
Մանրաչափային դաշտային տրանզիստորների նախագծում, պատրաստում և բնութագրում՝
առաջադեմ լիտոգրաֆիական տեխնոլոգիաների կիրառմամբ
Նախատեսվում է․ նախագծել, պատրաստել և բնութագրել մանրաչափային դաշտային տրանզիստորներ՝
առաջադեմ հաղորդիչ (ածխածնային նանոխողովակ և գրաֆեն)
բարձր k-ով մեկուսիչ նյութի՝ HfO₂ (կամ Al₂O₃) օգտագործմամբ։
Այս նյութերը ապահովում են ավելի լավ փականային կառավարում, նվազ արտահոսքային հոսանք և բարձրփոխահաղորդականություն՝ բարելավելով տրանզիստորի աշխատանքը նանոչափային տիրույթներում։

## Slide 31: Պատրաստման ընթացքը CEITEC-ում
Կոնտակտների նախագծում
ֆոտոլիտոգրաֆիայի կիրառմամբ (5մկմ)
Էլեկտրոնաճառագայթային լիտոգրաֆիայի կիրառմամբ (50-500նմ)

## Slide 32
Արդյունքներ
100 նմ բնութագրական չափերով ոսկու կոնտակտային սանրեր պատրաստված էլեկտրոնաճառագայթայինն վիմագրմամբ
5 մկմ բնութագրական չափերով ոսկու կոնտակտային սանրեր պատրաստված ֆոտովիմագրմամբ

## Slide 33: Conferences and activities 2025
New Trends in Chemistry
2025
Laboratory courses

## Slide 34
Six members of our group have completed an internship at the CEITECH Nano Center.

## Slide 35
Visit of International partnerof the project and signed the memorandum of understanding between the institutes FZU and ICHPH

## Slide 36
Prof. Dr. Hirakawa Kazuhiko, Institute of Industrial Science (IIS) University of Tokyo
Quantum Semiconductor Electronics Laboratory Hirakawa Group
**H-index 53
Prof. Dr. Artem Badasyan
University of Nova Gorica, Slovenia
**H-index 13
Prof. Dr. Arshak Poghossian
FH Aachen University of Applied Sciences · Institute of Nano- and Biotechnologies
**H-index 49
Prof. Dr. Michael Schoening
FH Aachen University of Applied Sciences ·
Director of the Institute of Nano- and Biotechnologies
**H-index 64
Alexander Dejneka, Ph.D
Institute of Physics of the Czech Academy of Sciences
Head of the Division of Optics, Head of the Department of Optical and Biophysical Systems
**H-index 36
Michal Urbánek, Ph.D
Brno University of Technology
(CEITEC BUT)
Head of CEITEC
Nano Research Infrastructure
**H-index 10

## Slide 37: Collaborations and resources
Institute of Nano-biotechnologies, FH Aachen, Germany
CEITEC, Central European Institute of Technology, Czech Republic
FZU, The Institute of Physics, Czech Republic
Ruder Boskovic institute, Croatia
Nova Gorica University, Slovenia

## Slide 38
International Colaboration
Erasmus+ 2023-1-SI01-KA171-HED-000122882
Key Action 1: -- Mobility for learners and staff -- Higher Education Student and Staff Mobility; participants: Yerevan State University and A.B. Nalbandyan Institute of Chemical Physics (IChPh) NAS RA , Armenia; University of Nova Gorica (UNG), Slovenia, UNG coordinator A. Badasyan, IChPh coordinator M. Yeranosyan 2026.
NATO Science for Peace and Security (SPS)
Programme SPS-supported Multi-Year Projects ։ Towards personalizedenvironmental UVmonitoring using quantumcomplex oxide films․
Advanced Functional Thin Film Processing and PLD Technology Development
Industrial R&D Collaboration with Huawei
Research and Development (R&D) of advanced functional thin-film deposition technologies
Selection and optimization of suitable carrier materials for target fabrication
Prototype target manufacturing and process validation
Development and optimization of Pulsed Laser Deposition (PLD) process parameters
Arrangement and optimization of deposition tools, vacuum systems, and supporting hardware
Prototyping of advanced functional thin-film samples by the ICNT research team
Experimental deposition trials and technology development for high-quality thin films and coatings
Thin-film testing and characterization
Iterative process optimization based on characterization feedback and engineering analysis
Technical reporting, process documentation, packaging, and delivery of developed samples
Project Outcome
Development of advanced PLD-based fabrication technology and prototyping workflow for next-generation multifunctional thin-film systems and industrial applications.

## Slide 40
Շնորհակալություն