## Slide 1
Double-Transition Metals MXenes as electrodes of supercapacitors: A DFT study
Hamidreza Jouypazadeh
Postdoctoral Researcher
Computational Materials Science Lab
The Center of Materials Science and Nanotechnology
Yerevan State University

## Slide 2
Introduction

## Slide 3: Capacitors VS. Batteries
Capacitors
Batteries
High power density
(low charging and discharging time)
High lifecycle
Low energy density
Low power density
(high charging and discharging time)
Low lifecycle
High energy density

## Slide 4
Ragone plot for different energy storage devices

## Slide 6
Supercapacitors

## Slide 7
Electric Double-Layer
Capacitors (EDLC)
Pseudo Capacitors
(PC)
Storing the charge via double layer formation at electrode/electrolyte interface
Excellent electrochemical stability
Excellent rate performance
Better charge-transfer kinetics
Storing the charge based on the rapid redox reactions at the surface or near surface
Storing higher charge than double-layer capacitors (10-100 times)

## Slide 8
Porous Carbon: surface area: 1500 m2/g
Cdl = 30-70 µF/cm2 CSC=4-5 µF/cm2
This limitation is originated from the Density of States near Fermi level
Density of States near Fermi level Quantum Capacitance
The Capacitance of EDLC

## Slide 9
Quantum Capacitance
Differential Quantum Capacitance:

## Slide 10
Total energy storage capacitance is based on integrated value over a complete charge-discharge cycle
Integrated Quantum Capacitance:

## Slide 11: 2D transition metal carbides, nitrides, and carbonitrides
MXenes
M. Naguib, M. Kurtoglu, V. Presser, J. Lu, J. Niu, M. Heon, L. Hultman, Y. Gogotsi and M. W. Barsoum, Advanced Materials, 2011, 23, 4248–4253.

## Slide 12
DTM Mxenes
Mx-yM’yXx-1Tx
.Anasori, Y. Xie, M. Beidaghi, J. Lu, B. C. Hosler, L. Hultman, P. R. Kent, Y. Gogotsi and M. W. Barsoum, ACS nano, 2015, 9, 9507–9516.

## Slide 13
Background
MXenes
VxCx-1Ty
MoxCx-1Ty
TixCx-1Ty
ZrxCx-1Ty
ScxCx-1Ty
DTM
MXenes
Zr2MC2O2
ScHfCO2
Cr2/3Sc1/3CO2
Mo2Ti2C3O2

## Slide 14
Our work
Mo-Ti
  MoTiC
  Mo2TiC2
  Ti2MoC2
  Mo2Ti2C3
  Ti2Mo2C3
Mo-V
  MoVC
  Mo2VC2
  V2MoC2
  Mo2V2C3
  V2Mo2C3
Ti-V
  TiVC
  Ti2VC2
  V2TiC2
  Ti2V2C3
  V2Ti2C3

## Slide 16
Results

## Slide 17
MoxTiyCx+y-1
MoxVyCx+y-1
TixVyCx+y-1
Structures of the DTM MXenes

## Slide 18
Stability
10 ps AIMD: small fluctuation in Energy
Undeformed Geometry
Phonon dispersion: No Imaginary modes observed
Elastic Constants: stiffer than corresponding mono-TM Mxenes
Mxenes three and four TM layer are as stiff as graphene

## Slide 19
Electronic Properties
Mo2Ti2C3
Mo2V2C3
Ti2V2C3

## Slide 20
MoxTiyCx+y-1
quantum capacitance

## Slide 21
quantum capacitance
MoxVyCx+y-1

## Slide 22
quantum capacitance
TixVyCx+y-1

## Slide 23
Conclusion

## Slide 24
Mo-Ti DTM MXenes:
The peak of quantum capacitance: 641.39 to 1051.76 μF/cm2 in aqueous electrolytes 641.39 to 1053.79 μF/cm2 in ionic/organic systems.
The highest quantum capacitance: Ti2Mo2C3 under negative bias (cathode)

## Slide 25
Mo-V DTM Mxenes
Mo2VC2, V2MoC2, Mo2V2C3, and V2Mo2C3 reaching peak values of 979.49 to 1521.08 μF/cm2 in ionic/organic electrolytes under positive bias (anode) except for V2MoC2
In aqueous electrolytes: 665.54 to 1117.17 μF/cm2
  Mo2VC2, and V2MoC2: cathode
  Mo2V2C3, and V2Mo2C3: anode

## Slide 26
Ti-V DTM MXenes:
The Top quantum capacitance of Ti2V2C3 reaches 1443.40 μF/cm2 across ionic/organic and 1323.85 at aqueous electrolyte types (anode).
The top quantum Capacitance of V2Ti2C3 exceeds 1200 μF/cm2 in negative bias (cathode)

## Slide 27
Thanks for your attention
Thanks For Your Attention…